Table 1: LA-ICP-MS analyses of some mineral phases of Sample 784

Table 2a: EDX composition of ilmenite in wt%. Phase labels: Figure No./the phase marked with a number in the BSE images. *Low cation numbers come from significant Nb-Ta-content causing high vacancy in position A; however, this very high Nb-Ta content is very atypical in ilmenite, probably submicroscopic Nb-Ta oxides were measured with ilmenite. **Cation numbers are too high in the B and too low in the A position, possibly indicating the transition of ilmenite into rutile

| Phase | 4/5* | 4/9* | 8/1** |
| --- | --- | --- | --- |
| P2O5 |  | 6.21 |  |
| Nb2O5 | 24.43 | 17.54 |  |
| Ta2O5 | 18.34 | 14.01 |  |
| TiO2 | 24.29 | 22.19 | 63.21 |
| UO2 |  | 1.63 |  |
| Al2O3 | 2.43 | 4.19 |  |
| MnO | 2.35 | 3.96 | 2.82 |
| FeO | 27.45 | 28.97 | 33.97 |
| CaO | 0.71 | 1.30 |  |
| Total | 100.00 | 100.00 | 100.00 |
| Cation numbers based on 3 oxygens |  |  |  |
| P |  | 0.14 |  |
| Nb | 0.31 | 0.21 |  |
| Ta | 0.14 | 0.10 |  |
| Ti | 0.51 | 0.44 | 1.13 |
| U |  | 0.01 |  |
| Al | 0.08 | 0.13 |  |
| ΣB | 1.04 | 1.03 | 1.13 |
| Mn | 0.06 | 0.09 | 0.06 |
| Fe | 0.65 | 0.64 | 0.68 |
| Ca | 0.02 | 0.04 |  |
| ΣA | 0.73 | 0.77 | 0.74 |

Table 2b: EDX composition of rutile in wt%. Phase labels: Figure No./the phase marked with a number in the BSE images

| Phase | 4/4 | 4/5 | 4/13 | 4/14 | 4/15 | 5/1 | 5/2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| WO3 | 7.84 |  |  |  | 2.05 | 5.48 | 5.49 |
| Nb2O5 | 10.78 | 7.00 | 6.06 | 2.25 | 12.23 | 5.77 | 5.74 |
| Ta2O5 | 6.07 | 20.95 | 3.45 |  | 3.02 |  |  |
| SiO2 |  |  | 2.54 | 0.70 |  | 1.02 | 1.15 |
| TiO2 | 67.89 | 64.03 | 84.51 | 95.50 | 76.92 | 80.56 | 80.57 |
| ZrO2 |  |  |  |  |  | 0.37 | 0.49 |
| SnO2 | 1.01 |  |  |  |  | 1.37 | 1.25 |
| UO2 |  |  |  |  |  | 0.34 | 0.33 |
| Al2O3 |  |  |  |  |  | 0.59 | 0.60 |
| Y2O3 |  |  |  |  |  | 0.18 |  |
| CaO |  |  |  |  |  |  | 0.13 |
| FeO | 6.41 | 8.02 | 3.44 | 1.55 | 5.77 | 3.70 | 3.70 |
| PbO |  |  |  |  |  | 0.61 | 0.55 |
| Total | 100.00 | 100.00 | 100.00 | 100.00 | 99.99 | 99.99 | 100.00 |
| Cation numbers based on 2 oxygens |  |  |  |  |  |  |  |
| W | 0.03 |  |  |  | 0.01 | 0.02 | 0.02 |
| Nb | 0.07 | 0.05 | 0.04 | 0.01 | 0.08 | 0.04 | 0.04 |
| Ta | 0.03 | 0.09 | 0.01 |  | 0.01 |  |  |
| Si |  |  | 0.04 | 0.01 |  | 0.01 | 0.02 |
| Ti | 0.78 | 0.77 | 0.88 | 0.96 | 0.84 | 0.87 | 0.86 |
| Zr |  |  |  |  |  | 0.00 | 0.00 |
| Sn | 0.01 |  |  |  |  | 0.01 | 0.01 |
| U |  |  |  |  |  | 0.00 | 0.00 |
| Al |  |  |  |  |  | 0.01 | 0.01 |
| Y |  |  |  |  |  | 0.00 |  |
| Ca |  |  |  |  |  |  | 0.00 |
| Fe | 0.08 | 0.11 | 0.04 | 0.02 | 0.07 | 0.04 | 0.04 |
| Pb |  |  |  |  |  | 0.00 | 0.00 |
| Total | 1.00 | 1.02 | 1.01 | 1.00 | 1.01 | 1.00 | 1.00 |

Table 2b continued: *too high total cation number possibly means a mixture with submicroscopic grains of a Mn-Fe-Zn rich phase, maybe pyrophanite

| Phase | 5/5 | 5/6 | 5/8* | 7/1 | 7/2 | 7/3 | 9/2 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| SO3 |  |  |  | 0.20 |  |  |  |
| WO3 |  | 1.62 |  | 0.58 |  |  |  |
| P2O5 |  |  |  | 3.50 | 4.27 |  |  |
| Nb2O5 | 2.31 | 4.15 | 3.23 | 24.93 | 18.99 | 24.75 | 1.68 |
| Ta2O5 |  | 1.76 | 2.46 | 2.31 | 3.73 | 2.81 |  |
| SiO2 |  |  | 3.19 | 4.16 | 9.43 | 5.59 |  |
| TiO2 | 96.66 | 88.87 | 64.75 | 53.09 | 46.70 | 53.36 | 98.32 |
| SnO2 |  | 1.04 |  |  |  |  |  |
| ThO2 |  |  |  | 0.13 | 0.62 | 1.13 |  |
| UO2 |  |  |  | 0.33 |  | 0.98 |  |
| Al2O3 |  | 0.35 |  | 2.48 | 3.20 | 2.62 |  |
| Y2O3 |  |  |  |  | 1.47 |  |  |
| Nd2O3 |  |  |  |  | 0.28 |  |  |
| Sm2O3 |  |  |  |  | 0.30 |  |  |
| Gd2O3 |  |  |  |  | 0.44 |  |  |
| Er2O3 |  |  |  |  | 0.38 |  |  |
| Yb2O3 |  |  |  |  | 0.26 |  |  |
| MgO |  |  |  |  |  | 0.41 |  |
| CaO |  |  |  | 0.32 | 0.46 | 0.10 |  |
| MnO |  |  | 13.93 |  |  | 0.04 |  |
| FeO | 1.03 | 2.21 | 5.23 | 5.27 | 6.06 | 7.21 |  |
| ZnO |  |  | 7.21 |  |  |  |  |
| PbO |  |  |  | 1.72 | 1.52 |  |  |
| Na2O |  |  |  | 0.57 | 0.60 | 0.64 |  |
| K2O |  |  |  | 0.41 | 1.30 | 0.35 |  |
| Total | 100.00 | 100.00 | 100.00 | 100.00 | 100.01 | 99.99 | 100.00 |
| Cation numbers based on 2 oxygens |  |  |  |  |  |  |  |
| S |  |  |  | 0.00 |  |  |  |
| W |  | 0.01 |  | 0.00 |  |  |  |
| P |  |  |  | 0.04 | 0.05 |  |  |
| Nb | 0.01 | 0.03 | 0.02 | 0.16 | 0.12 | 0.17 | 0.01 |
| Ta |  | 0.01 | 0.01 | 0.01 | 0.01 | 0.01 |  |
| Si |  |  | 0.05 | 0.06 | 0.14 | 0.08 |  |
| Ti | 0.98 | 0.93 | 0.75 | 0.58 | 0.51 | 0.60 | 0.99 |
| Sn |  | 0.01 |  |  |  |  |  |
| Th |  |  |  | 0.00 | 0.00 | 0.00 |  |
| U |  |  |  | 0.00 |  | 0.00 |  |
| Al |  | 0.01 |  | 0.04 | 0.05 | 0.05 |  |
| Y |  |  |  |  | 0.01 |  |  |
| Nd |  |  |  |  | 0.00 |  |  |
| Sm |  |  |  |  | 0.00 |  |  |
| Gd |  |  |  |  | 0.00 |  |  |
| Er |  |  |  |  | 0.00 |  |  |
| Yb |  |  |  |  | 0.00 |  |  |
| Mg |  |  |  |  |  | 0.01 |  |
| Ca |  |  |  | 0.01 | 0.01 | 0.00 |  |
| Mn |  |  | 0.18 |  |  | 0.00 |  |
| Fe | 0.01 | 0.03 | 0.07 | 0.06 | 0.07 | 0.09 |  |
| Zn |  |  | 0.08 |  |  |  |  |
| Pb |  |  |  | 0.01 | 0.01 |  |  |
| Na |  |  |  | 0.02 | 0.02 | 0.02 |  |
| K |  |  |  | 0.01 | 0.02 | 0.01 |  |
| Total | 1.00 | 1.03 | 1.16 | 1.00 | 1.02 | 1.04 | 1.00 |

Table 2c: EDX composition of columbite-tantalite in wt%. Phase labels: Figure No./the phase marked with a number in the BSE images

| Phase | 4/1 | 4/2 | 4/3 | 4/7 | 5/7 |
| --- | --- | --- | --- | --- | --- |
| Nb2O5 | 42.11 | 55.92 | 46.63 | 17.30 | 59.34 |
| Ta2O5 | 24.74 | 10.49 | 21.52 | 51.78 | 4.58 |
| TiO2 | 9.78 | 7.45 | 7.48 | 11.91 | 10.89 |
| SnO2 |  | 0.15 |  |  | 1.02 |
| Sc2O3 | 0.25 | 0.25 | 0.37 | 0.38 | 0.57 |
| Y2O3 | 1.24 | 1.14 | 1.58 | 1.15 | 1.44 |
| Sm2O3 |  |  | 0.20 |  |  |
| Gd2O3 |  |  | 0.41 | 0.15 |  |
| Ho2O3 |  |  |  |  | 0.23 |
| Er2O3 | 0.23 | 0.31 | 0.47 | 0.61 | 0.41 |
| Yb2O3 | 0.46 | 1.20 | 1.02 | 0.59 | 0.89 |
| Lu2O3 | 0.45 | 0.47 | 0.68 | 0.18 | 0.17 |
| MgO | 0.56 | 0.31 |  |  |  |
| CaO | 0.22 | 0.28 | 0.38 |  | 0.77 |
| MnO | 9.11 | 9.04 | 5.88 | 5.66 | 7.72 |
| FeO | 10.77 | 12.89 | 13.30 | 10.07 | 11.83 |
| Total | 99.92 | 99.90 | 99.92 | 99.78 | 99.86 |
| Cation numbers based on 6 oxygens |  |  |  |  |  |
| Nb | 1.16 | 1.47 | 1.29 | 0.53 | 1.50 |
| Ta | 0.41 | 0.17 | 0.36 | 0.96 | 0.07 |
| Ti | 0.45 | 0.33 | 0.34 | 0.61 | 0.46 |
| Sn |  | 0.00 |  |  | 0.02 |
| Sc | 0.01 | 0.01 | 0.02 | 0.02 | 0.03 |
| Y | 0.04 | 0.04 | 0.05 | 0.04 | 0.04 |
| Sm |  |  | 0.00 |  |  |
| Gd |  |  | 0.01 | 0.00 |  |
| Ho |  |  |  |  | 0.00 |
| Er | 0.00 | 0.01 | 0.01 | 0.01 | 0.01 |
| Yb | 0.01 | 0.02 | 0.02 | 0.01 | 0.02 |
| Lu | 0.01 | 0.01 | 0.01 | 0.00 | 0.00 |
| ΣB | 2.09 | 2.06 | 2.11 | 2.18 | 2.15 |
| Mg | 0.05 | 0.03 |  |  |  |
| Ca | 0.01 | 0.02 | 0.02 |  | 0.05 |
| Mn | 0.47 | 0.45 | 0.30 | 0.33 | 0.37 |
| Fe | 0.55 | 0.63 | 0.68 | 0.57 | 0.55 |
| ΣA | 1.08 | 1.13 | 1.00 | 0.90 | 0.97 |

Table 2d: EDX composition of other accessory minerals in wt%. Phase labels: Figure No./the phase marked with a number in the BSE images. n.d. = non detected.

Formulae:

4/8: (Ca0.89Na0.70Al0.36Fe0.14Pb0.05Mn0.02)Σ=2.16 (Ta1.46Nb0.25Ti0.21Sn0.03U0.01)Σ=1.96 O6 (F0.51O0.49)Σ=1.00.

4/12: (Zr0.68Hf0.14Si0.11Al0.05Fe0.03Ti0.01)Σ=1.02 Si1.00 O4.

5/3: (Sn0.84Ti0.13Nb0.02Fe0.02)Σ=1.01 O2.

9/1 Ca1.00 (Ca0.27Ce0.24La0.14Nd0.10)Σ=0.75 Al2.00 (Fe0.64Al0.38)Σ=1.02 Si3.15 O12 (OH).

| Phase | 4/8 | 4/12 | 5/3 | 9/1 |
| --- | --- | --- | --- | --- |
| Mineral | fluorcalcio-microlite | zircon | cassiterite | allanite-(Ce) |
| Nb2O5 | 6.57 |  | 1.52 |  |
| Ta2O5 | 64.58 |  | 0.62 |  |
| SiO2 |  | 35.84 |  | 37.27 |
| TiO2 | 3.29 | 0.60 | 7.24 |  |
| ZrO2 |  | 45.40 |  |  |
| SnO2 | 0.83 |  | 89.84 |  |
| HfO2 |  | 15.62 |  |  |
| UO2 | 0.45 |  |  |  |
| Al2O3 | 3.69 | 1.48 |  | 23.96 |
| La2O3 |  |  |  | 4.35 |
| Ce2O3 |  |  |  | 7.84 |
| Nd2O3 |  |  |  | 3.48 |
| CaO | 9.97 |  |  | 14.01 |
| MnO | 0.25 |  |  |  |
| FeO | 2.02 | 1.06 | 0.78 | 9.09 |
| PbO | 2.06 |  |  |  |
| Na2O | 4.36 |  |  |  |
| H2O | n.d. |  |  | n.d. |
| F | 1.92 |  |  |  |
| –O = F | –0.81 |  |  |  |
| Total | 99.18 | 100.00 | 100.00 | 100.00 |

Table 2e: EDX composition of some undefined Ti-Nb-Y-(Fe)-oxide minerals in wt%. Phase: Figure No./the phase marked with a number in the BSE images.

| Phase | 4/10 | 4/11 | 5/4 | 5/9 |
| --- | --- | --- | --- | --- |
| P2O5 | 3.99 | 3.41 |  |  |
| Nb2O5 | 22.11 | 26.77 | 34.59 | 21.21 |
| Ta2O5 | 10.66 | 9.08 | 2.32 | 1.47 |
| SiO2 |  |  |  | 2.53 |
| TiO2 | 27.81 | 25.57 | 23.54 | 33.49 |
| ThO2 |  |  |  | 0.79 |
| UO2 | 1.28 | 0.59 | 0.19 | 1.34 |
| Al2O3 | 3.64 | 2.78 |  | 1.21 |
| Y2O3 | 8.67 | 11.83 | 17.35 | 11.24 |
| Ce2O3 |  |  | 0.86 | 11.07 |
| Nd2O3 | 1.58 | 1.97 | 2.45 | 4.60 |
| Sm2O3 | 1.84 | 2.45 | 3.27 |  |
| Gd2O3 |  | 2.47 | 3.45 | 2.21 |
| Dy2O3 |  |  | 6.60 | 2.24 |
| Er2O3 |  |  | 1.95 |  |
| Yb2O3 |  |  | 1.11 | 1.24 |
| CaO | 1.64 | 1.80 | 2.33 | 2.56 |
| MnO | 2.21 | 1.31 |  |  |
| FeO | 14.56 | 9.98 |  | 1.52 |
| Na2O |  |  |  | 1.17 |
| K2O |  |  |  | 0.12 |
| Total | 99.99 | 100.01 | 100.01 | 100.01 |

Table 3: Formulae of the Nb-Ta-bearing mineral phases with the measured replacements. *Possibly mixture of ilmenite and small inclusions of oxides and phosphates of these elements)

| Mineral phase | Formulae with common replacements | Analyzed other replacements (enriched occasionally) | Analytical method |
| --- | --- | --- | --- |
| rutile | (Ti,Fe,Nb,Ta)O2 | W, Sn, Al, P, Zn, Y, Mn, Zr | EDX |
| niobian ilmenite* | (Fe,Mn,Pb)(Ti,Nb,Ta,P,Al,U,Zr,Y,Ce)O3 | Zn, W, Th, Dy, Sm, Gd, Er, Ca, Ni | LA-ICP-MS, EDX |
| ilmenite | (Fe,Mn,Zn)(Ti,Ta,Nb)O3 | Al, Ni, Pb, Zr, Y | LA-ICP-MS |
| columbite-(Fe) | (Fe,Mn)(Nb,Ti,Ta)2O6 | Ca, Mg, W, Sn, Y | EDX |
| tantalite-(Fe) | (Fe,Mn)(Ta,Ti,Nb)2O6 | Y | EDX |
| fluorcalciomicrolite | (Ca,Na,Fe)2(Ta,Nb,Ti,Al)2O6F | Sn, Mn | EDX |
| cassiterite | (Sn,Ti,Fe,Nb,Ta)O2 |  | EDX |

Table 4: Major and trace element contents of samples of the BMR and the SMV (from SiO2 to TOTAL: wt%, from Sr to Lu: ppm, n. a. means non analyzed, EOV means Uniform National Projection System in Hungary)

Table 5: Detailed results of the laser ablation U-Pb geochronology